### ***MATERIAL SAFETY DATA SHEET***

ITEM NUMBER                              6390

- PRODUCT NAME:		NITRILE POLYMER COATED POWDER FREE GLOVES

- NON - STERILE

- TRADE NAME:			“Sanitex”

- MATERIAL:			100 % NITRILE -BUTADIENE COMPOUND

- FDA 510 (K) NO:		Not Required

- FDA 2892 NO:			Not Required

REGISTRATION NO:		2086535

- IATA/IACO HAZARD RATING:	NOT RESTRICTED

D.O.T. RATING:			NOT RESTRICTED

ASTM STANDARD:		ASTM D6319-99

1000cc WATER TIGHT TEST:      NOT PERFORM.

SAMPLING PLAN:                         S-2, ABOUT AQL 2.5

# SPECIFICATION

| Size / Item # | S / #6392 | M / #6393 | L / #6394 | XL / #6395 |
| --- | --- | --- | --- | --- |
| Length (mm) / inch | 240 / 9.5” | 240 / 9.5” | 240 / 9.5” | 240 / 9.5” |
| Width at Palm (mm) | 85±5 | 95±5 | 105±5 | 115±5 |
| Thickness at finger mm (mil) | 0.10 (4 mil) | 0.10 (4 mil) | 0.10 (4 mil) | 0.10 (4 mil) |
| Thickness at palm mm (mil) | 0.08 (3.5 mil) | 0.08 (3.5 mil) | 0.09 (4 mil) | 0.09 (4 mil) |
| Thickness at Cuff mm (mil) | 0.075 (3 mil) | 0.075 (3 mil) | 0.075 (3 mil) | 0.075 (3 mil) |

PROPERTIES

|  | BEFORE AGING | AFTER AGING* |
| --- | --- | --- |
| TENSILE STRENGTH | Minimum 21 Mpa | Minimum 19 MPa |
| ULTIMATE ELONGATION | 700 % | 680 % |

*(N.B. Accelerated aging at 70+/-2 degrees centigrade for 166+/-2 hrs.)

| Coating Material | Polyurethane Polymer |
| --- | --- |
| ORIENTATION | Ambidextrous, Full Textured |
| CUFF | Round beaded cuff |
| COLOR | Blue |

FIRE AND EXPLOSION

| Stability | Flash Point | Extinguishing Media | Conditions to Avoid | Incompatible Material |
| --- | --- | --- | --- | --- |
| Stable | N/A | Foam, Water, CO2 | Extreme Heat | None |

PACKAGING		100 pieces per box, 10 dispenser boxes per 20-lb case, 100 cases/pallet.

STORAGE		Store at room temperature.  Keep away from heat.

Avoid direct sunlight and fluorescent light.

CAUTION	*Immediately discontinue use if reactions are suspected.

*Not intended for use as a general chemical barrier.

*Safe use of this glove by or on latex sensitive individuals

has not been established.

05/2008